## Slide 1
Manipulating Polymers with Light Activated Chemistries for Patterning Films and Manufacturing Fibers
Christopher J. Ellison
McKetta Department of Chemical Engineering
and Texas Materials Institute
The University of Texas at Austin
ellison@che.utexas.edu
Notes: 1

## Slide 2: Acknowledgements
Welch Foundation (F-1709)
NSF CAREER (DMR-1053293)
ACS PRF 49881-DNI7
3M Nontenured Faculty Award
DuPont Young Professor Award

## Slide 3
Fibers: From Clothing to Advanced Materials
Clothing
Technical textiles
http://inventors.about.com/od/pstartinventions/ss/Parachute_7.htm
http://www.nationalfirefighter.com/index.php?cPath=6
http://www.mcrsafety.com/index.php/gloves/products/kevlar_gloves
http://www.archiexpo.com/prod/afitex/nonwoven-geotextiles-for-drainage-1588-306972.html
http://articles.textileclass.com/medical-textiles-manufacturers-companies-who-produce-medical-fabrics/
http://www.medicaldevice-network.com/features/feature731/feature731-1.html
http://www.engadget.com/2010/07/13/mits-piezoelectric-fibers-can-act-as-speaker-or-microphone-don/
http://www.danbru.com/blog/?blog=plastic-optical-fiber-comeback
Synthetic grafts, surgical aids, tissue engineering scaffolds
Piezoelectric fibers
Plastic optical fibers

## Slide 4
Conventional (> 10 microns)
Melt extrusion / spinning
Solution spinning
Current Polymer Fiber Manufacturing
Advanced (10 nm to 10 microns)
Electrospinning (electric fields)
Melt blowing (hot air jets)
Forcespinning™ (centrifugal forces)
Solvent recovery/recycling or thermal energy input
Critical sustainability challenges
Solvents or heat
+ processing
Bulk polymer
Fibers
Processing preformed polymers (long chain molecules) into fibers.
Substantial use of solvent or heat: a necessity to lower viscosity for processing.
Can we make fibers without any solvent or heat??
http://www.fiber-science.com/fswp002.htm
http://www.globaltextiles.com/manufacturers
Notes: Restricting to polymer derived fibers
Whether it is conventional fiber manufacturing used to make microfibers or advanced fiber manufacturing methods used to make nanofibers
Unifying theme is use of organic volatile solvents or heat input is a necessity in fiber manufacturing.
This is because

## Slide 5
Hyoung-Joon Jin and David L. Kaplan, Nature, 2003, 424, 1057-1061
Intricate self-assembly of protein constituents during the fiber formation process
The science of spider silk formation is evolving
A sophisticated biochemistry to understand and mimic
Nature’s Approach
Spiders and Silkworms
Mechanically strong and tough fibers
Made in a benign way
Notes: Can we make fibers without any solvent or heat ?? Nature has the answer.
Looking at silk fiber production by spiders and silkworms
Have a benign way of making mechanically strong and tough fibers through an intricate self-assembly of protein constituents during the fiber formation process
Obtaining a complete and fundamental understanding of this biosynthetic process, or engineering synthetic silk fibers with equivalent mechanical properties, is an open challenge in the field.

## Slide 6: Bio-inspired Approach
Start with small molecules and build long chain structures in real time
Concept of simultaneous polymerization and extrusion
Spiders silk spinning rate : 1-10 cm/s
Synthetic fiber extrusion speeds (melt blowing, etc.) : > 1 m/s
Need extremely fast and robust polymerization chemistry
Chemistry of Thiol-ene Photopolymerization
K. B. Guess, C. Viney, Thermochim. Acta 1998, 315, 61.
Fast kinetics under ambient conditions (room T in air)
Only requires addition of a light source to existing fiber equipment
Notes: Viewed broadly, nature’s approach of chemically linking small functional units into long chain molecules and solid fibrillar structures while simultaneously extruding the fibers is fundamentally different from current synthetic fiber manufacturing methods, where extrusion of pre-formed long chain polymers is facilitated with organic solvent or heat.
Can we broadly adapt nature‘s approach to make fibers without solvents or heat
The main challenge is to find chemistries by which one can rapidly mediate interactions between the functional units within the time scale of extrusion.

## Slide 7: Simultaneous Reaction and Extrusion
Desireable attributes:
Fast polymerization rates in air
Can be low shrinkage at high conversion
Network homogeneity
Wide choice of thiol and -ene monomers
Other uses:
Nanoimprinting
Dental restorative materials
Extracellular matrix mimics
Hydrogels for protein delivery
Gas transport membranes
Thiol-ene Photopolymerization:
A Step-growth Polymerization Under Some Circumstances
Hoyle et al., J. Polym. Sci. Pol. Chem. 2004, 42, 5301.Hagberg et al., Nano Lett. 2007, Lu et al., Dent. Mater. 2005, 21, 1129. Fairbanks et al., Adv. Mater. 2009, 21, 5005,Aimetti et al., Biomaterials 2009, 30, 6048, Kwisnek et al., Macromolecules 2009, 42, 7031.
Notes: Under some circumstances thiol-ene photopolymerization proceeds in a step growth

## Slide 8
Thiol-ene Fiber Process: Solventless and Heatless
Dipentaerythritol Pentaacrylate (DPPA)
Pentaerythritol tetrakis (3-mercaptopropionate) (PETT)
200 W metal halide w/LLG and collimating lens, ~200 mW/cm2
Syringe pump
Grounded collector
High voltage supply
monomers
Onset of photocuring
Solid photo-cured fibres
Challenges:
Matching curing kinetics with high velocity of spinning
Available curing time < 0.5 secs
1.02 mm ID needle
Irgacure 2100
Notes: Our approach was to conduct in-situ photopolymerization of thiol and ene monomers during fiber spinning.
We used a multifunctional acrylate and thiol compound.
It is important to note these have very low vapor pressure. Boiling points above 300 C or so.
Integrating thiol-ene photopolymerization and electrospinning into a simultaneous process presents several operational challenges. The curing kinetics must be matched to the speed of the high velocity fluid jet moving towards the collector.
Reported (Reneker et al.) jet velocity is ~0.5 m/s. We have estimated our average jet velocity at the collector as ~1 m/s, based on known feed rates and typical starting and final fiber diameters. Considering this speed and the distance between the needle tip and-collector, the available time for photopolymerizing the thiol-ene fluid jet in-situ is ~0.1 s.
Choosing mulitfunctional monomers for faster kinetics

## Slide 9: First Generation of Thiol-ene Fibers
Pentaerythritol tetrakis (3-mercaptopropionate) (PETT) and dipentaerythritol pentaacrylate (DPPA) in 1:4.4 thiol to ene ratio along with 6wt% Irgacure 2100TM as photoinitiator.
Solid continuous fibers reproducibly obtained at 1:4.4 ratio of thiol to ene groups in spinning mixture
Molar ratio of thiol:ene groups critical
Influences both curing kinetics and viscosity of spinning fluid
C.J. Ellison and K. Shanmuganathan, Patent application (PCT/US12/32465) filed .
K. Shanmuganathan, R. Sankhagowit, P.Iyer and C.J. Ellison, Chem. Mater., 2011, 23 (21), 4726–4732
Notes: Low and high magnification SEM images of thiolene fibers made by photopolymerization of pentaerythritol tetrakis (3-mercaptopropionate) and dipentaerythritol pentaacrylate in a 1:4.4 thiol to ene ratio along with 6wt% Irgacure 2100 as photoinitiator.

## Slide 10
.
1:3.4 ratio of thiol to ene
Discontinuous and partially cured fibers
Less thiol
More thiol
1:5.6 ratio of thiol to ene
Continuous but partially cured fibers
Fiber quality: A delicate balance of photocuring kinetics and viscoelastic properties of the spinning mixture
Importance of Thiol to Ene Ratio
C.J. Ellison and K. Shanmuganathan, Patent application (PCT/US12/32465) filed .
K. Shanmuganathan, R. Sankhagowit, P.Iyer and C.J. Ellison, Chem. Mater., 2011, 23 (21), 4726–4732
Notes: When the stoichiometry of thiol to ene is slightly altered, we observed quite significant changes in fiber morphology, such as partially cured discontinuous strands and other defects
SEM images of thiolene fibers made by photopolymerization of pentaerythritol tetrakis (3-mercaptopropionate) (PETT) and dipentaerythritol pentaacrylate (DPPA ) (a) in a 1:3.4 thiol to ene ratio and (b) in a 1:5.6 thiol to ene ratio along with 6wt% Irgacure 2100 as photoinitiator
a simultaneous interplay of several physical and chemical factors including fluid viscoelasticity, surface tension, electrostatic forces, and curing kinetics. For example, electrostatic repulsive forces tend to increase the surface area of the electrified jet originating from the needle tip, while surface tension can induce the elongated jet to break into spheres to minimize surface area; high viscosities can limit rapid diameter reduction while low viscosities facilitate it.

## Slide 11
1:4.4 ratio of thiol to ene provides fast kinetics in short time scales with a suitable viscosity
Viscosity and Curing Kinetics
C.J. Ellison and K. Shanmuganathan, Patent application (PCT/US12/32465) filed .
K. Shanmuganathan, R. Sankhagowit, P.Iyer and C.J. Ellison, Chem. Mater., 2011, 23 (21), 4726–4732
Increasing Thiol
Viscosity too low
Cure kinetics too slow
Notes: Fig (right) shows the photocuring kinetics of the different mixtures of thiol-ene described above. Though the final conversion of ene groups and the kinetics are roughly similar at first glance there is a significant difference at very short curing times, i.e., less than 2 seconds (right bottom). In this timescale, the mixture with a thiol to ene ratio of 1:4.4 cures faster compared to 1:3.4 or 1:5.6. Since the time available for curing the thiol-ene filament en route to the collector is fractions of a second, slight kinetic differences in this regime likely have significant impact on fiber quality.
Also the thiol monomer used here is less viscous than the ene monomer. The viscosity of the thiol-ene mixture with 1:4.4 ratio of thiol to ene groups that yielded high quality fibers is about 1.7 Pa-s. A lesser thiol to ene ratio (1:5.6) increases the viscosity to 2.1 Pa-s, while increasing the thiol content (1:3.4) decreases the viscosity to 1.3 Pa-s.
With more thiol (previous slide), viscosity of mixture is less. Hence surface tension forces dominate.
With less thiol, viscosity is sufficient to resist deformation but curing becomes slower.
Reducing the thiol content below a certain level can also reduce photocuring rates in air, and ultimately adversely affect final fiber quality. In traditional acrylate photopolymerizations, oxygen reacts with carbon radicals to form a peroxy radical. Peroxy radicals are less reactive than carbon radicals and therefore oxygen quenches the reaction. In a thiol-ene photopolymerization, the peroxy radical abstracts hydrogen from a thiol unit regenerating thiyl radicals making thiol-ene polymerizations less sensitive to oxygen. This feature is instrumental in performing this fiber forming process in ambient conditions and it could be an important controlling factor in fiber quality in some circumstances.

## Slide 12: Reactive Surfaces: Multifunctional Materials
Dipentaerythritol Pentaacrylate (DPPA)
Pentaerythritol tetrakis (3-mercaptopropionate) (PETT)
Bright field
Fluorescence
Thiolene fibers after reaction with fluorescent marker
Bright field
Fluorescence
Thiolene fibers before treatment with fluorescent marker
Josh Katzenstein
Notes: We are using a multifunctional monomers here. Some unreacted thiol and double bonds will exist in the photopolymerized fibers. We can monitor the conversion of both the thiol and double bonds using IR spectroscopy.
Fibers have about 40-50% unreacted thiol and double bonds
Attaching flourescent markers to fibers

## Slide 13
Fibers retain shape after heating up to 1000 C in nitrogen
Mesoporous structure:
10-200 nm pore size
Mesoporous Carbon Fibers
Negligible weight loss until above 350 C in inert atmosphere
Chemical and Thermal Stability
Thiol-ene fibers not soluble or fractured by swelling in THF or immersing in toluene at 50 C for 4 h
Notes: What’s more interesting is that the fibers retain shape even after heating to 1000C
These fibers show a mesoporous structure with pore size between 10-200 nm.

## Slide 14: Thermomechanical Stability of Thiol-ene Fibers
C.J. Ellison and K. Shanmuganathan, Patent application (PCT/US12/32465) filed .
K. Shanmuganathan, R. Sankhagowit, P.Iyer and C.J. Ellison, Chem. Mater., 2011, 23 (21), 4726–4732
    High thermomechanical stability
    (~10 GPa 25oC, > 3 GPa 200oC)
Stress-strain behavior of 3 fibers
8-12 % strain at break
Spider silk fibers from different spiders
Vollrath F and Knight DP, Nature, 2001, 410, 541-548
E‘ > 4 GPa at 50 C
> 1 GPa at 180 C
Notes: The fiber formation reported here relies on externally triggering covalent interactions between functional segments.
This has several significant advantages. The fibers have very good chemical stability because of the crosslinked molecular architecture formed during curing.
For example, thiol-ene fibers were not soluble or fractured by swelling in THF or toluene, which are good solvents for the ene and thiol precursors.
Further, the morphology of the fibers was unaffected even after immersing the fibers in toluene at 50 C for 4 hrs.
The fibers have very good thermal stability upto 400C indicating their crosslinked network architecture

## Slide 15
Stretchable Elastic Fibers and Nonwoven Mats
Fiber mechanical properties can be tuned by choice of chemistry
Irgacure 2100

## Slide 16
Chart: Time (min)
Chart: % Strain
Chart: Strain (%)
Chart: Strain (%)
Single fibers show good strength and ~ 40% elongation at break
Mechanical properties of nonwoven mat at ~90% porosity at room T
Mechanical properties show little degradation after strain cycling nonwoven mat to 40% strain
Nonwoven mats are robust at 200°C.
Stretchable Elastic Fibers and Nonwoven Mats

## Slide 17
Worldwide Production of Nonwoven Fibers*
  > 1 × 109 kg/year
  > 1 × 1010 $/year
  Biorenewable Polymers
    Poly(lactide) (PLA)
    Poly(trimethylene terepthalate)
Petroleum vs. Biorenewable Feedstocks
Acrylated Epoxidized Soybean Oil (AESO)
Inks/Coatings
(Webster Group, NDSU)
Sheet Molding Compound Resins (Wool Group, U. Del.)
Thermoset Foams (K.-Y. Lee et al. Green Chemistry, 2011)
USDA
© 3M 2012. All Rights Reserved.
*Lee and Cassill, Journal of Textile and Apparel, Technology and Management (2006)

## Slide 18
Soybean Oil Based Fibers
Fibers
51 wt. % AESO
29 wt. % DPPA
14 wt. % PETT
6 wt. % Irgacure 2100
Mn = 1138 g/mol, f = 2.7
Dipentaerythritol Pentaacrylate
Mn = 525 g/mol, f = 5
Pentaerythritol tetrakis(3-mercaptopropionate)
Mn = 489 g/mol, f = 4
C.J. Ellison et al, US Patent application filed .
D.W.Janes, K. Shanmuganathan, D.Y. Chou and C.J. Ellison, ACS Macro Letters, 2012, 1, 1138−1142.

## Slide 19
Chart: Temperature (o C)
2 o/min in N2
Soak in 80 oC Toluene for 5 h
Dry in vacuo
Soybean Oil Fibers – Thermochemical Stability

## Slide 20: Fiber Summary
A simple route to fiber manufacturing based on photopolymerization chemistry, which eliminates the need for using toxic solvents or heat energy.
    Insensitive to oxygen / can be conducted at room temperature in air
    Thermally (up to 400 oC) and chemically (hot toluene, etc.) stable fibers due to cross-linking
    High modulus over wide temperature range (~4 GPa 25oC, > 1 GPa 180oC)
    Multifunctionality can be exploited, many thiols and enes remaining
    Adaptable to all continuous spinning methods
    Nanofibers coming soon!
C.J. Ellison and K. Shanmuganathan, Patent application (PCT/US12/32465) filed .
K. Shanmuganathan, R. Sankhagowit, P.Iyer and C.J. Ellison, Chem. Mater., 2011, 23 (21), 4726–4732.
C.J. Ellison et al, US Patent application filed (soybean oil)
D.W.Janes, K. Shanmuganathan, D.Y. Chou and C.J. Ellison, ACS Macro Letters, 2012, 1, 1138−1142.

## Slide 21
Anti-Biofouling
http://www.sharklet.com
Neurite Guiding
Rajnicek, A. M.; Britland, S.; McCaig, C. D.
J. Cell Sci. 1997, 110, 2905-2913.
Photovoltaic Devices
Kim, JB, et al.,
Nat. Photonics 2012, 6, 327-332.
Micropatterning in Polymer Films - Applications
Wrinkles
Folds
Notes: Notes:
Neurite Guidance: The basic idea is that neurites preferentially align down grooves, in these images groves are 1 um wide and 320 nm deep (not too far out of our realm). They are made of quartz, but could imagine using our stuff to pattern these materials.
Photovoltaic devices: Top is wrinkles with 1.8 um period and peak to valley height of 180 nm. It is then compressed and the fractional area of the folds is 0.174. Under compression some of the wrinkles collapse by ‘self-contact’. Basically in the sharp line area stress has made the wrinkles stick together. (scale bar is 5 um)

## Slide 22
LISA/LISC
EHP
Chou, S. Y.; Zhuang, L.
J. Vac. Sci. Technol. B 1999, 17, 3197-3202
Schaffer, E.; et al.
Nature 2000, 403, 874-877
Polymers
Polymerizable Liquids
Dickey, M.; et al.
J. Mater. Sci. 2008, 43, 117-122.
Micropatterning in Polymer Films - Methods
Notes: LISA is image of PMMA, the top is the mask and the bottom is the transferred image. 530 nm pillar height, 1.6 um pillar diameter. Their model has localized positive charge formed by electrohydrodynamic instabilities rising toward the top plate. 130 °C for “5-80 mins” under vacuum. They say it doesn’t depend on heating time…though I’m not sure that makes sense.
EHP of polymers is a ‘brominated PS film (h=45 nm). Features are ~125 nm deep. Aspect ratio 0.83. Took 14 hours at 170 °C.
Polymerizable liquid is a thiol-ene reaction that started as a spin cast film of 800 nm.

## Slide 23
Photo credits:
http://www.flickriver.com/photos/selago/3388356089/
http://athome.harvard.edu/programs/stone/imageframe/37.html
http://www.coatings.rutgers.edu/Defects.htm
‘Tears’ of Wine
Thin Film Striations
The Marangoni Effect

## Slide 24
After 1 min. Light Exposure – Metal Halide Lamp
Chart: Position (μm)
Chart: Position (μm)
Light = Exposed
Dark = Unexposed
Topography Formation – Polystyrene (PS) Films
After 10 min. Heating
10 minute heating at 110 °C without mask
Mn = 2900 g/mol, PDI = 1.2
Tg = 61 °C by DSC

## Slide 25
Chart: 
UV light → backbone dehydrogenation
Formation of ‘stilbene-like’ units
Red shifted fluorescence compared to PS
  Solutions in THF
  ~0.05 mg/mL
Excitation wavelength = 310 nm
hν
Photochemical Dehydrogenation of PS
Blue = Neat PS
Red = Exposed PS
Fluorescence (a.u.)
Wavelength (nm)

## Slide 26
Conversion of PS to partially-dehydrogenated analog (diamonds) increases with UV exposure dose
  Measured by FTIR
  Filled point represents typical dose and conversion: 1 minute exposure
Surface chemistry changes qualitatively measured by water contact angle (squares)
Photochemical Dehydrogenation of PS
Conversion (%)
Contact Angle (°)
Dose (J/cm2)*
hν
*Note: Dose is measured as intensity of entire output spectrum
of lamp including wavelengths PS does not absorb.
Chart: 
| 0 | 420 | 840 | 1260 | 1680 | 2100 | 2520
Conversion | 0 | 3.0881 | 6.398 | 8.1187 | 11.3512 | 13.2314 | 14.7105
Contact Angle | 90.6 | 88.8
Notes:   FTIR: Disappearance of methylene in backbone, normalized by carbonyl in initiator fragment (ATRP – EBIB)

## Slide 27
Chart: Conversion (%)
  = Surface energy change with composition
  H = Characteristic length (half pitch)
  CPS = Concentration of PS
  = Viscosity
  = Diffusion coefficient
Critical value for instabilities = 801
  Critical conversion: 0.02%
  Actual conversion: 6.4%
Ma in this system ~ 20000
  Orders of magnitude above critical value
1) Reichenbach, J.; Linde, H. J. Colloid Interface Sci. 1981, 84, 433-443.
Critical Conversion
The Marangoni Number

## Slide 28
Other Photochemical Effects?
Chart: Binding Energy (eV)
XPS:
No Oxidation
Unexposed = Dashed
Exposed = Solid
O 1s
Chart: Elution Volume (mL)
SEC:
No Chain Coupling Events
Unexposed = •
Exposed = ■

## Slide 29
Patterns directly from photomasks
Profilometery trace follows dark line
Features go either direction
  Up = Exposed
  Down = Protected
Scale bars = 30 μm
Pattern Diversity - Direct Pattern Transfers

## Slide 30
Large Bumps
Small Bumps
‘Dogbones’
‘Lines-in-Lines’
Same Mask Rotated 90° 2nd Exp.
Different Masks
Multiple line-and-space mask exposures
Development step after all exposures completed
Pattern Diversity - Multiple Exposures
Notes: Large Bumps: 12.5 μm chrome lines on a 25 μm pitch
Small bumps: 5 μm chrome lines on a 10 μm pitch
Two on right:
First exposure: 12.5 μm chrome lines on a 25 μm pitch photomask
Second exposure: 5 μm lines on a 10 μm pitch photomask

## Slide 31
Lines
Arbitrary Shapes
Topographic Feature Formation
Notes: Ticker in corner is real time at development temperature.

## Slide 32
Terms:
  h = Film Height
  𝛤0 = Mean Surface Energy
  μ = Viscosity
  h0 = Initial Film Thickness
Introduced a surface energy that varies in position and time
Model of Marangoni Flow Process
)
Transient Film Height
Visco-Capillary
Forcing
Marangoni Forcing
Chart: Time at 120 °C (min)
| 0 | 10 | 15 | 20 | 25 | 30 | 40 | 50 | 60 | 70 | 80 | 90 | 100 | 120 | 140 | 150 | 170 | 190 | 210 | 230 | 250 | 270 | 300 | 330 | 360 | 390 | 420 | 480 | 540 | 600 | 720
Data | 0 | 0.2089 | 0.29579 | 0.39265 | 0.46124 | 0.5463 | 0.66661 | 0.74303 | 0.77232 | 0.83947 | 0.88547 | 0.89631 | 0.93752 | 0.96758 | 1 | 0.98728 | 0.96415 | 0.98306 | 0.98198 | 0.95875 | 0.9396 | 0.90986 | 0.84048 | 0.82042 | 0.75987 | 0.72663 | 0.68042 | 0.59388 | 0.54558 | 0.47757 | 0.4096
Model | 0 | 0.17243 | 0.25002 | 0.32223 | 0.38935 | 0.45163 | 0.56265 | 0.65715 | 0.73683 | 0.80322 | 0.85772 | 0.90161 | 0.93604 | 0.98065 | 0.99885 | 0.99996 | 0.98942 | 0.96544 | 0.9316 | 0.89079 | 0.84534 | 0.79706 | 0.72245 | 0.64828 | 0.57692 | 0.50984 | 0.4479 | 0.34064 | 0.25502 | 0.18856 | 0.1002
With Roger Bonnecaze

## Slide 33
Summary and Future Directions
Marangoni-driven flow is a powerful technique for patterning polymer films
  Directed topography formation driven by surface energy gradients from patterned photochemistry
Versatile and potentially high throughput method
Continuing to study mechanism
  Modeling
  Kinetic parameters
Can this be applied to other polymers?
Nanoscale patterns?
C.J. Ellison et al, US Patent application filed (Marangoni patterning).
J.M. Katzenstein, D.W. Janes, J.D. Cushen, N.B. Hira, D.L. McGuffin, N.A. Prisco and C.J. Ellison, ACS Macro Letters, vol 1, pg 1150, 2012.
D.W. Janes, J.M. Katzenstein, K. Shanmuganathan and C.J. Ellison, J. Polym. Sci.: Polym. Phys., vol 51, pg 535, 2013.